| FACILITY: |  | Chinchaga Plant PLT/c-032-H/094-H-08/00 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | PROV. REG. N0: |  |  |  |  | 570539 |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| EQUIPMENT NAME: |  |  | Process Boiler Steam Generator |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | TAG NO: |  |  | 603FB001 |  |  |  |  |  |  |  |  |  |  |  |
| SIZE: | 1524 mm |  |  | ID x |  | 3962 mm |  |  | L/H |  |  |  | L |  |  |  |  |  | MAWP: |  |  | 1379 kpa |  |  |  |  |  |  |  |  | kPa @ |  | 343 | C |
| ITEM INSPECTED: Shell, Coil, Burner, Refractory, Insulation, Anchors, Manway. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | MANWAY |  |  |  |  |  | YES |  |  |  | NO |  |  |  |  |  |
| SERVICE: sour sweet cryogenic |  |  |  |  |  |  |  |  |  |  |  |  |  |  | FLUID: Glycol/Fuel Gas |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| SCOPE OF INSPECTION |  |  |  |  |  |  | TYPE OF INSPECTION: |  |  |  |  |  |  |  |  |  | CLEANING: |  |  |  |  |  |  |  |  |  |  | ACCESS: |  |  |  |  |  |  |
| PRECOMMISSIONING |  |  |  |  |  |  | AE | MT |  | RT |  |  |  |  |  |  | GOOD |  |  |  |  |  |  |  |  |  |  | FULL |  |  |  |  |  |  |
| INITIAL |  |  |  |  |  |  | ET | MFL |  | UT |  |  |  |  |  |  | FAIR |  |  |  |  |  |  |  |  |  |  | PARTIAL |  |  |  |  |  |  |
| REINSPECTION |  |  |  |  |  |  | LT | PT |  | VT |  |  |  |  |  |  | INADEQUATE |  |  |  |  |  |  |  |  |  |  | EXTERNAL |  |  |  |  |  |  |
|  |  |  |  |  |  |  | OTHER |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PLEASE ADD PAGES AND SKETCHES AS NEEDED (TURN OVER FOR SKETCH) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| OBSERVATIONS: |  |  |  |  |  |  | EXTERNAL |  |  |  | INTERNAL |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Internal: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Small loose metal slag noted around manway. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| All anchors in place throughout vessel, anchors secure and showing no indication of degradation. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Coils tight and showing no signs of distortion, or indications of corrosion or mechanical damage. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Minor loose deposits between coils of insulation debris between the 11 coils at the burner end. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Refractory showing 4 thin cracks with no spalling at 12, 2, 5 and 10 O'clock. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Inner Rim refractory: Various refractory chips at 4, 5, 7-11. 0.150" Loss. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Outter Rim refractory: Various chips 10-3, largest section missing at 5 O'clock 45mm Wide x 115mm long x 15mm deep. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| No exposed components through refractory. No detached pieces found in boiler. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Insulation clean and intact throughout. No visible components exposed. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Burner Assembly clean and secure. Burner tip clean and intact. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Manway gasket intact. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Signs of hot gas leakage at 12 O'clock on manway. Previously fixed with what appears to be application of HT Silicone. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| RECOMMENDATIONS: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Return to service, monitory manway for hot gasses and seal appropriately, reinspect at appropriate interval. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| UT performed by Rob Kassian, no low readings noted, report to follow. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| SUITABLE FOR FURTHER SERVICE: |  |  |  |  | YES |  |  | NO |  |  |  |  |  | REMEDIAL ACTION PRIORITY: |  |  |  |  |  |  |  | HIGH |  |  |  | MEDIUM |  |  |  |  |  | LOW |  |  |
| INSPECTION PERFORMED BY: |  |  |  |  |  | Kevin Gawley, Reviewed Will Rettman |  |  |  |  |  |  |  |  |  |  |  |  |  |  | DATE OF INSPECTION : |  |  |  |  |  |  |  |  | July 17, 2012 |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | (DAY-MONTH-YEAR) |  |  |  |  |
| FOLLOW-UP INSPECTION REQ’D: |  |  |  |  |  |  |  |  |  |  |  | YES |  |  |  | NO |  |  |  |  | BY DATE: : |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | (DAY-MONTH-YEAR) |  |  |  |  |

1) External Overview of Vessel:

2) Manway towards Burner End Overview: (Liquid at 12, 3, 6 and 9 O’clock: UT Couplant)

3) Slag and Debris around Manway; No visibly degraded sections of metal observed:

4) Minor bits of loose insulation noted between 11 coils at burner end: :

5) Burner End Overview: :

6) Representative crack on refractory: :

7) Refractory Overview:

8) Missing Refractory :

7) Burner Assembly Overview:

5) Burner End towards Manway Overview:

7) Manway Cover:

5) Hot Gas Leak: