	[image: image1.jpg]ConocoPhillips



                                                                         Pressure Equipment Integrity

	Version 1.0 released April 2008                                                               

	GENERAL INSPECTION FORM

	District: Northern Plains
	Skid No. : 16718

	Facility: Fire Bird Oil Battery
	Location (LSD) Surface: 14-01-98-08-W6M

	Vessel Name & Equipment Number: Horizontal Treater

	Orientation:  Horizontal   FORMCHECKBOX 
      or     Vertical    FORMCHECKBOX 

	Location (LSD) Downhole:

	Status:   In Service   FORMCHECKBOX 
   or   Out of Service (blinded / fully isolated)   FORMCHECKBOX 
   
	Commissioning Inspection  FORMCHECKBOX 
   or    Regulatory Inspection   FORMCHECKBOX 


	PRESSURE VESSEL NAMEPLATE DATA

	“A" or “G” or “S” (Sask.) or BC Registration Number. 

A2738569
	CRN Number
K-5298.2

	Vessel serial number: 
HT-6605
	Size (diameter x length- estimate if necessary):   
96 in X 30 ft S/S        

	Shell thickness: 7.9 mm
	Shell material:  SA-516-70N

	Head thickness: 13.0 mm / 10.4 mm  
	Head material:  SA-516-70N

	Tube wall thickness: 
	Tube material: 

	Tube diameter: 
	Tube length: 

	Channel thickness: 
	Channel material:  

	MAWP
	Shell: 50 Psi
	Operating pressure
	Shell: 

	
	Tubes: 
	
	Tubes: 

	Design Temp.
	Shell: 200 F
	Operating temperature
	Shell: 

	
	Tubes:  
	
	Tubes: 

	X-ray: RT-3
	Heat treatment?  No

	Code parameters: ASME VIII, Div 1
	Joint efficiency (if on nameplate): 

	Manufacturer:  Larsen & D’Amico
	Year built:  1991

	Corrosion allowance: 1.6 mm
	Manway?    Yes  20 in 

	PRESSURE SAFETY VALVE NAMEPLATE DATA

	Tag Number(s)
	Set Pressure
	CRN #
	Manufacturer/ Model / Serial /  Code Stamp
	Capacity (Scfm)
	Size (Inlet x Outlet)
	Set Date

(mm/dd/yyyy)

	Shell Side G#

705459
	50 Psi
	
	Crosby, Jos-15-A, sn- SE-6026-1
UV, NB
	3535 SCFM
	3” #150 X 4” #150
	7/3/2006

	Tube Side G#


	
	
	
	
	
	

	SERVICE CONDTIONS-INDICATE ALL THAT APPLY

	Sweet     FORMCHECKBOX 

	Sour      FORMCHECKBOX 

	Oil      FORMCHECKBOX 

	Gas     FORMCHECKBOX 

	Water   FORMCHECKBOX 


	Amine     FORMCHECKBOX 

	LPG      FORMCHECKBOX 

	Condensate      FORMCHECKBOX 

	Air       FORMCHECKBOX 

	Glycol  FORMCHECKBOX 


	Other (Describe):


Inspection Interval ________________________________________PSV Service Interval_________________________________

(Determined by integrity specialist in conjunction with Chief Inspector following guidelines of ConocoPhillips Canada Owner-User Inspection Program)
Reports reviewed and accepted by:

Integrity Specialist________________________________________________________Date_____________________________
Fill out all forms as completely as possible. All information is important!  Use back of sheets to record additional information or sketch if required.

	Pressure Equipment Integrity Management Program
	This document contains proprietary information belonging to ConocoPhillips Canada and must not be wholly or partially reproduced nor disclosed without written prior permission from ConocoPhillips Canada.
	Page 1


	External Inspection Items
	G
	F
	P
	N/A
	Comments

	Insulation Verify sealed around manways, nozzles, no damage present, and there is no egress of moisture. Are straps secure?
	
	
	
	X
	Vessel is not insulated.

	External Condition Assess paint condition, areas peeling, record any corrosion, damage, distortion etc (record location, size and depth of corrosion or damage)
	X
	
	
	
	No scratches or peeling of pain external surface. Vessel is suited with a 20” #150 man way closure, davit arm appears to be in good condition with no visible damage.

	Leakage Record any leakage at flanges, threaded joints, weep holes on repads, etc.
	
	
	
	X
	No leaks.

	Skirt/ Saddle    Assess condition of paint, fire protection, concrete. Look for corrosion, buckling, dents, etc. Look at vessel surface area near supports. Verify no signs of leakage at attachment to vessel and attachment welds are acceptable. Is ground wire attached?
	X
	
	
	
	Saddles are seal welded to shell, weld appears full and complete.
No distortion – no buckles or dents – no obvious leaks at shell to saddle welds.
Vessel is grounded directly.

	Anchor Bolts    Hammer tap to ensure secure. Look for corrosion, cracking in threads or signs of deformation.
	X
	
	
	
	In Place and secure

	Concrete foundation Check for cracks, spalling, etc. 
	
	
	
	X
	

	Ladder / Platform    Describe general condition, ensure support is secure to vessel, describe any hazards. 
	
	
	
	X
	 

	Nozzle Assess paint, look for leakage, and ensure stud threads are fully engaged. Record any damage, deflection, etc. Are nozzles gusseted? Inspect gussets for cracking.
	X
	
	
	
	All nozzles are clean with no visible deflection noted. 
Paint condition is good – no exposed metal.

	Gauges Ensure gauges are visible, working, no leakage, and suitable for range of MAWP/ Temp.
	X
	
	
	
	Pressure and temperature gauge attached - Acceptable ranges.

	External Piping  Ensure pipe is well supported. All clamps, supports, shoes, etc. in place. Look for evidence of structural overload, deflection, etc. Paint condition, external corrosion?
	X
	
	
	
	All external piping is well supported with no visible deflection or signs of any leakage present at time of inspection.

	Valving  Ensure no leaks are visible. Valves are properly supported and chained if necessary.
	X
	
	
	
	Well supported – no leaks.

	PSV Ensure PSV is set at pressure at or below that of vessel. Discharge piping is same size as valve outlet and is properly supported and routed.  Are psv seals in place? Ensure no block valves between psv and vessel, or if there are ensure they are locked/sealed open.
	X
	
	
	
	Located on top shell - set at the vessel MAWP.
Seal intact.

No block valve.

Discharge piping same size as outlet orifice.

	NDE methods Was UT/ MPI done on vessel

	X
	
	
	
	Ultrasonic thickness inspection carried out, piping metal thickness detected below nominal minus corrosion allowance. Critical thickness calculations carried out - insufficient metal exits for safe operation.

	Other Observations:

See internal inspection for summary and recommendations.


Inspected By: Jerald Zaderey                                                                                                                                    Date: July 28, 2008

 (Please Print)

	Pressure Equipment Integrity Management Program
	This document contains proprietary information belonging to ConocoPhillips Canada and must not be wholly or partially reproduced nor disclosed without written prior permission from ConocoPhillips Canada.
	Page 2


	Internal Inspection Items
	G
	F
	P
	N/A
	Comments

	Coating Assess coating. Describe area coated, general condition of coating. Look at nozzles, coupling, and areas of most severe corrosion to ensure coating is intact. If coating is in poor condition make decision now if re-coating necessary? If so, when?
	
	X
	
	
	The internal coating is in good condition with only 6 minor coating chips that are believed to have been caused by mechanical cleaning. All are patch coated. The coating is starting to blister on the down comer seal pan, no visible corrosion is present at time of inspection. 

	Anodes. How many, type, condition. % consumed. Are they being replaced?
	
	X
	
	
	The anodes located in the vessel were found to be 25% to 75% gone. It is suggested the doubling up the anodes may help, also to monitor anode usage to determine usage. 

	Internal Piping Is there any? If so, carbon or stainless steel. Describe condition, dents, corrosion, erosion, etc. Ensure supports are secure and any bolts are suitable for future use.
	X
	
	
	
	All internal piping and non pressure containing parts within the treater were found to be in good clean condition with no visible damage or anomalies present. The fire tubes were removed and MPI completed on all welds, cracks were detected and require to be repaired. Completed by Natco Canada

	Trays How many? Type of material. Are valves in place. Check for erosion/ corrosion; wear on tray valve legs. Cleanliness?
	
	
	
	X
	

	Baffles, deflector plates, etc. If present, describe condition. Look closely at welds attached to vessel wall. 
	X
	
	
	
	All are securely attached with no concerns noted at time of inspection.

	Bottom Head Note all corrosion, erosion or mechanical damage. (If vessel is horizontal identify direction of this head)
	X
	
	
	
	North head found to be in good clean condition with no coating defects noted.

	Top Head Note all corrosion, erosion or mechanical damage. (If vessel is horizontal identify direction of this head)
	X
	
	
	
	South head has two burner tube openings and is found to be in good clean condition with some minor coating defects noted on the burner opening edges. These will be repaired prior to placement of vessel back into service.

	Shell Sections Record number of shell sections. Record location, size and depth of all erosion, corrosion or mechanical damage. Describe general condition.  If any corrosion greater than corrosion allowance is observed in either shell or head, discuss with Chief Inspector before closing vessel.
	X
	
	
	
	 The entire shell is found to be in good clean condition with a few minor coating chips noted. No visible corrosion noted.

	Demister pad Is it in place? Is it clean? If any corrosion is apparent in vessel, lift pad and check top head for corrosion.
	
	
	
	X
	No demister pad.

	Welds Inspect all welds, including attachment welds. Record all service-related damages and if there is any discuss with Chief Inspector before closing.
	X
	
	
	
	All welds appear to be full and complete with no coating failures noted.

	Repairs Required. If yes, ensure procedure and copy of AB-40 is on file, and one sent to local ABSA Inspector


	X
	
	
	
	1. Weld repair cracks in fire tube flange to tube. Natco repaired cracks that were detected in the fire tubes along the flange.
2. Change out corroded water dump piping.



	NDE Was any NDE done. 


	X
	
	
	
	Magnetic Particle Inspection carried out on fire tube welds – both fire tube detected with cracking at flange to tube. 

	Other Observations

Recommendations: 1. Replace all thin and corroded piping as identified on RTD Quality Services Corrosion survey report. 2. Weld repair fire tube cracks. 3. Replace anodes.
Summary: This vessel is in good condition, visual external and internal carried out – a few small chips in the coating, no corrosion or pitting to vessel internal. Both fire tubes detected with cracks in flange to tubes. Water dump piping found corroded to 50% wall loss.

Fire tube was repaired, all cracks removed and weld build up completed by Natco Canada.
Vessel is fit to be returned back into service.


Inspected By: Jerald Zaderey                                                                                                                                    Date: July 28, 2008






(Please Print)

	Pressure Equipment Integrity Management Program
	This document contains proprietary information belonging to ConocoPhillips Canada and must not be wholly or partially reproduced nor disclosed without written prior permission from ConocoPhillips Canada.
	Page 3


Photo Table

	[image: image2.jpg]


  
Nameplate
	 [image: image3.jpg]


 
Vessel External Over View

	 [image: image4.jpg]


 
Anode As Found Condition
	[image: image5.jpg]


 
Fire Tubes

	[image: image6.jpg]



Coating damage on inlet deflector seal pan.
	 


[image: image7.jpg]ConocoPhillips



