	Canadian Natural Resources Limited

GENERAL PRESSURE VESSEL INFORMATION

	District: Fort St. John, B.C.
	Skid No.

	Facility: Clear Hills Gas Field
	Location (LSD): 3-22-88-12-W6M

	Vessel Name Equipment Number: 3 Phase Separator

	Orientation: Vertical 

	Status:         In Service
	   Regulatory Inspection  

	PRESSURE VESSEL NAMEPLATE DATA

	“A” or “G” or “S” (Sask.) or BC Registration Number.

A2847104
	CRN Number:

K 9276.21

	Vessel serial number: 30234-200
	Size: 16in.x 86in

	Shell thickness: 26.19mm
	Shell material: SA 106-B

	Head thickness: 20.93mm
	Head material: Sa 516-70N

	Tube wall thickness:
	Tube material:

	Tube diameter:    
	Tube length:  

	Channel thickness:    
	Channel material: 

	Design pressure
	Shell:   9929 KPa
	Operating pressure
	Shell:        0 – 6800 KPa

	
	Tubes:     
	
	Tubes:     

	Design Temp.
	Shell:      38 Deg.C  
	Operating temperature
	Shell:      -40 – 50 Deg C

	
	Tubes:        
	
	Tubes:                                                 

	X-ray: RT-2
	Heat treatment: no

	Code parameters: ASME VIII, Div 1 
	Coated:   no

	Manufacturer: NUSCO
	Year built:1994

	Corrosion allowance: 1.59mm
	Manway: no

	PRESSURE SAFETY VALVE  NAMEPLATE DATA

	PSV Tag  #
	Manufacture
	Model #
	Serial #
	Set Pressure

(kPa)
	Capacity

(scfm)
	Service

Date

	1622 F
	Taylor
	T-8200-1
	69553-37
	1440 PSI
	5181
	03/05

	CRN #
	Service By
	Block Valve
	Location
	Size
	Code Stamp
	

	OG 1316.1234
	unified valve
	no 
	upper shell
	1”x 1”
	UV
	

	SERVICE CONDITIONS-INDICATE ALL THAT APPLY

	  Sweet   X
	Sour  
	 Oil   
	Gas   X 
	Water  X

	 Amine
	LPG    
	Condensate   X
	Air  
	Glycol  

	Other (Describe):    


Inspection Interval ________________________________________PSV Service Interval_________________________________

(Determined by MIC in conjunction with Chief Inspector following guidelines of  CNRL’s Owner-User Inspection Program)
Reports reviewed and accepted by:
Mechanical Integrity Coordinator________________________________________________Date__________________________

Fill out all forms as completely as possible. All information is important!  Use back of sheets to record additional information or sketch if required.

Copy of report to be filed by MIC at site, and copy sent to Chief Inspector

	External Inspection Items


	G
	F
	P
	N/A
	                    Comments



	Insulation Verify sealed around manways, nozzles, no damage present, and there is no egress of moisture.
	
	
	
	X
	Vessel not insulated

	External Condition  Assess paint condition, areas peeling, record any corrosion, damage, etc (record location, size and depth of corrosion or damage)
	X
	
	
	
	Paint peeling 30% of area.
Scale and corrosion where paint has peeled – no pitting.



	Leakage Record any leakage at flanges, threaded joints, weep holes on repads, etc.
	X
	
	
	
	No leaks observed

	Saddle/Skirt Assess condition of paint, fire protection, concrete. Look for corrosion, buckling, dents, etc. Look at vessel surface area near supports. Verify no signs of leakage at attachment to vessel and attachment welds are acceptable. Ground wire attached?
	X
	
	
	
	Skirt:
Welded directly to skid floor.

No buckling or dents.

Paint peeling to 80% of area.

No ground wire attached to vessel or skid

	Anchor Bolts    Hammer tap to ensure secure. Look for cracking in treads or signs of deformation.
	
	
	
	X
	Vessel welded to skid floor

	Concrete foundation Check for cracks, spalling, etc. 
	
	
	
	X
	

	Ladder / Platform    Describe general condition, ensure support is secure to vessel, describe any hazards. 
	
	
	
	X
	

	Nozzle Assess paint, look for leakage, and ensure stud threads are fully engaged. Record any damage, deflection, etc. Are nozzles gusseted?
	X
	
	
	
	Threaded nozzle joints are fully engaged.
No leaks observed.

No damage or deflection.

Nozzles are not gusseted

	Gauges Ensure gauges are visible, working, no leakage, and suitable for range of MAWP/ Temp.
	X
	
	
	
	Gauges are clear and clean. No leakage.
Pressure gauge not suitable for range of MAWP of vessel

Pressure gauge 0 – 6800 KPa/ temperature gauge -40 -50Deg. C

	External Piping Ensure pipe is well supported. All clamps, supports, shoes, etc. in place. Look for evidence of structural overload, deflection, etc. Paint condition, external corrosion?
	X
	
	
	
	Piping is well supported.
Clamp missing on inlet piping at support

No structural overloads or deflections

Paint peeling to 40% of area.

	Valving Ensure no leaks are visible. Valves are properly supported and chained if necessary.
	X
	
	
	
	No leaks are visible.
Valve is properly supported

	PSV Ensure PSV is set at pressure at or below that of vessel. 
	X
	
	
	
	Located on upper shell - set at MAWP of vessel.

No block valve – seal intact.

	NDE methods Was UT/ MPI done on vessel
(MI coordinator to review results)
	X
	
	
	
	Ultrasonic thickness inspection carried out – piping metal thickness detected below nominal minus corrosion allowance. Calculations carried out to ensure sufficient metal exists for safe operation.

	Recommendations or corrective actions :  Vessel is Fit for  Service or describe corrective actions required)
(MIC to review corrective actions with Operations, discuss with Chief Inspector where necessary, and get remedial action implemented)

Recommendations: 1. Install ground cable to skid. 2. Clean up external and paint.
Summary: This vessel is in good condition, visual external and ultrasonic thickness testing carried out - piping metal thickness detected below nominal minus corrosion allowance. Calculations carried out to ensure sufficient metal exists for safe operation.
Vessel is fit for service.


Inspected By: Gerry Avery                                                                                                                                  Date: August 28, 2007
Photo Table

	[image: image1.jpg]11| I¥iINusCO R

\ — L LUUNISKUSALBERTA, CANADA

§ W £ . MAX: ALLOW
RT 2 WORK: PRESS.

MIN: DESIGN
METAL TEMP.

SERIAL i i
;N.o. L0012 04 =220

f pnass rl 440




	[image: image2.jpg]




	 vessel data plate
	vessel temperature gauge

	[image: image3.jpg]



	[image: image4.jpg]




	vessel pressure gauge
	  vessel skirt welded to skid floor

	[image: image5.jpg]



	

	vessel overview
	

	
	

	
	


















































