	Canadian Natural Resources Limited

GENERAL PRESSURE VESSEL INFORMATION

	District:   Fort St. John, B.C.
	Skid No.    

	Facility:   Clear Hills Gas Field
	Location (LSD):  08-23-87-12-W6M 

	Vessel Name Equipment Number:  3 Phase Separator

	Orientation:  Vertical

	Status:          In Service
	   Regulatory Inspection  

	PRESSURE VESSEL NAMEPLATE DATA

	“A” or “G” or “S” (Sask.) or BC Registration Number.

A2763857
	CRN Number:

K 9068.2

	Vessel serial number:  6000E-V01
	Size:  16 in. x 84 in

	Shell thickness:     12.7 mm  
	Shell material:   SA 106-B    

	Head thickness:     12.7 mm 
	Head material:   SA 516-70N    

	Tube wall thickness:     
	Tube material:    

	Tube diameter:    
	Tube length:        

	Channel thickness:    
	Channel material:     

	Design pressure
	Shell:        4964 kPa
	Operating pressure
	Shell:    0 – 7000 KPa    

	
	Tubes:     
	
	Tubes:     

	Design Temp.
	Shell:        49 °C
	Operating temperature
	Shell:    -40 – 50 Deg. C  

	
	Tubes:       
	
	Tubes:                                                 

	X-ray:   RT-1                        
	Heat treatment: yes   

	Code parameters:   ASME VIII, Div 1  
	Coated: no              

	Manufacturer:   NUSCO  
	Year built: 1993        

	Corrosion allowance: 3.2 mm    
	Manway:   no         

	PRESSURE SAFETY VALVE NAMEPLATE DATA

	PSV Tag  #
	Manufacture
	Model #
	Serial #
	Set Pressure

(kPa)
	Capacity

(scfm)
	Service

Date

	Not Stated 
	Taylor
	T8200-2
	56692-78
	4964
	6186
	03/05

	CRN #
	Service By
	Block Valve
	Location
	Size
	Code Stamp
	

	
	Unified valve 
	No
	Upper shell
	2”x 2”
	UV
	

	SERVICE CONDITIONS-INDICATE ALL THAT APPLY

	  Sweet   
	Sour  X
	 Oil   
	Gas   X  
	Water  X

	 Amine
	LPG    
	Condensate  X  
	Air  
	Glycol  

	Other (Describe):    


Inspection Interval ________________________________________PSV Service Interval_________________________________

(Determined by MIC in conjunction with Chief Inspector following guidelines of CNRL’s Owner-User Inspection Program)
Reports reviewed and accepted by:
Mechanical Integrity Coordinator________________________________________________Date__________________________

Fill out all forms as completely as possible. All information is important!  Use back of sheets to record additional information or sketch if required.

Copy of report to be filed by MIC at site, and copy sent to Chief Inspector

	External Inspection Items


	G
	F
	P
	N/A
	                    Comments



	Insulation Verify sealed around manways, nozzles, no damage present, and there is no egress of moisture.
	
	
	
	X
	Vessel not insulated

	External Condition  Assess paint condition, areas peeling, record any corrosion, damage, etc (record location, size and depth of corrosion or damage)
	X
	
	
	
	 Paint peeling to 80% of area.
Pit corrosion where paint has peeled. Depth of pits .010”- .070”

	Leakage Record any leakage at flanges, threaded joints, weep holes on repads, etc.
	X
	
	
	
	No leaks observed

	Saddle    Assess condition of paint, fire protection, concrete. Look for corrosion, buckling, dents, etc. Look at vessel surface area near supports. Verify no signs of leakage at attachment to vessel and attachment welds are acceptable. Ground wire attached?
	X
	
	
	
	Skirt:
Skirt bolted directly to skid floor.

No buckling or dents 

No corrosion at attachment welds to vessel.

Ground wire attached to skid package

	Anchor Bolts    Hammer tap to ensure secure. Look for cracking in treads or signs of deformation.
	X
	
	
	
	Anchor bolts are securely fastened to skid floor.
No deformation

	Concrete foundation Check for cracks, spalling, etc. 
	
	
	
	X
	

	Ladder / Platform    Describe general condition, ensure support is secure to vessel, describe any hazards. 
	
	
	
	X
	

	Nozzle Assess paint, look for leakage, and ensure stud threads are fully engaged. Record any damage, deflection, etc. Are nozzles gusseted?
	X
	
	
	
	Threaded nozzle joints are fully engaged.
No leaks observed.

No damage or deflections.

Nozzles are not gusseted

	Gauges Ensure gauges are visible, working, no leakage, and suitable for range of MAWP/ Temp.
	X
	
	
	
	Gauges are clear and clean.
Suitable for range of MAWP/Temperature of vessel.

Temperature gauge: -40 – 50 Deg. C/pressure 0 – 7000 KPa

	External Piping Ensure pipe is well supported. All clamps, supports, shoes, etc. in place. Look for evidence of structural overload, deflection, etc. Paint condition, external corrosion?
	X
	
	
	
	Piping well supported. All clamps and supports are in place.
No structural overloads or deflections.
Paint peeling 90% of area. Corrosion on piping where paint peeled

	Valving Ensure no leaks are visible. Valves are properly supported and chained if necessary.
	X
	
	
	
	No leaks are visible.
Valves are properly supported

	PSV Ensure PSV is set at pressure at or below that of vessel. 
	X
	
	
	
	Located on upper shell - set at MAWP of vessel.
Seal intact – no block valve.

	NDE methods Was UT/ MPI done on vessel
(MI coordinator to review results)
	X

	
	
	
	 Ultrasonic thickness survey carried out – shell and head metal thickness detected below nominal. Calculations carried out to ensure sufficient metal exists for safe operation.

	Other


	
	
	
	
	

	Recommendations or corrective actions :  Vessel is Fit for  Service or describe corrective actions required)
(MIC to review corrective actions with Operations, discuss with Chief Inspector where necessary, and get remedial action implemented)

Recommendations: 1. Re-paint vessel
Summary: This Vessel is in good overall condition, ultrasonic thickness survey carried out – shell and head metal thickness detected below nominal. Calculations carried out to ensure sufficient metal exists for safe operation.

Vessel is fit for service                                                                                                                                                                                                                                


Inspected By:  Gerry Avery 








          Date: June 21, 2007

	[image: image1.jpg]e ) R ‘ \ it l{
| MIN.DESIGN |
R R ! META'QTEM 1\





	[image: image2.jpg]




	             Vessel data plate
	            Vessel temperature gauge

	[image: image3.jpg]



	[image: image4.jpg]




	      Vessel pressure gauge
	            Corrosion where paint peeled

	[image: image5.jpg]



	[image: image6.jpg]




	           Corroded piping
	                Vessel overview








