	Canadian Natural Resources Limited

GENERAL PRESSURE VESSEL INFORMATION

	District: Fort St. John, BC.
	Skid No.

	Facility: Clear Hills Gas Field
	Location (LSD): )  01-35-87-13-W6M

	Vessel Name Equipment Number: 3 Phase Separator

	Orientation: Vertical

	Status:         In Service
	   Regulatory Inspection  

	PRESSURE VESSEL NAMEPLATE DATA

	“A” or “G” or “S” (Sask.) or BC Registration Number.

A 2763864
	CRN Number:

K 9068.21

	Vessel serial number: 6000F-VOI
	Size: 14in.x 90in

	Shell thickness: 12.7mm
	Shell material: SA 106-B

	Head thickness: 12.7mm
	Head material: SA 516-70N

	Tube wall thickness:
	Tube material:

	Tube diameter:    
	Tube length:  

	Channel thickness:    
	Channel material: 

	Design pressure
	Shell:   720 PSI
	Operating pressure
	Shell:    0 – 1000 PSI  

	
	Tubes:     
	
	Tubes:     

	Design Temp.
	Shell:    120 Deg F
	Operating temperature
	Shell:      

	
	Tubes:        
	
	Tubes:                                                 

	X-ray: RT1
	Heat treatment: yes

	Code parameters: ASME VIII, Div 1 
	Coated:   no

	Manufacturer: NUSCO
	Year built: 1997

	Corrosion allowance:3.2mm
	Manway: no

	PRESSURE SAFETY VALVE NAMEPLATE DATA

	PSV Tag  #
	Manufacture
	Model #
	Serial #
	Set Pressure

(kPa)
	Capacity

(scfm)
	Service

Date

	
	Taylor
	T-7900-2
	not stated
	720 PSI
	2994
	03/05

	CRN #
	Service By
	Block Valve
	Location
	Size
	Code Stamp
	

	not stated
	unified valve
	no
	upper shell
	2”x 2”
	UV
	

	SERVICE CONDITIONS-INDICATE ALL THAT APPLY

	  Sweet   
	Sour  X
	 Oil   
	Gas  X  
	Water  X

	 Amine
	LPG    
	Condensate   X
	Air  
	Glycol  

	Other (Describe):    


Inspection Interval ________________________________________PSV Service Interval_________________________________

(Determined by MIC in conjunction with Chief Inspector following guidelines of CNRL’s Owner-User Inspection Program)
Reports reviewed and accepted by:
Mechanical Integrity Coordinator________________________________________________Date__________________________

Fill out all forms as completely as possible. All information is important!  Use back of sheets to record additional information or sketch if required.

Copy of report to be filed by MIC at site, and copy sent to Chief Inspector







	External Inspection Items


	G
	F
	P
	N/A
	                    Comments



	Insulation Verify sealed around manways, nozzles, no damage present, and there is no egress of moisture.
	
	
	
	X
	Vessel not insulated

	External Condition  Assess paint condition, areas peeling, record any corrosion, damage, etc (record location, size and depth of corrosion or damage)
	X
	
	
	
	Paint in good condition. 
No exposed metal

	Leakage Record any leakage at flanges, threaded joints, weep holes on repads, etc.
	X
	
	
	
	No leaks observed

	Saddle/Skirt Assess condition of paint, fire protection, concrete. Look for corrosion, buckling, dents, etc. Look at vessel surface area near supports. Verify no signs of leakage at attachment to vessel and attachment welds are acceptable. Ground wire attached?
	X
	
	
	
	Skirt: Bolted directly to skid floor
No buckling or dents.

No corrosion at attachment welds to vessel.

Paint in good condition.

Ground wire attached to skid 

	Anchor Bolts    Hammer tap to ensure secure. Look for cracking in treads or signs of deformation.
	X
	
	
	
	Anchor bolts are securely fastened to skid floor

	Concrete foundation Check for cracks, spalling, etc. 
	
	
	
	X
	

	Ladder / Platform    Describe general condition, ensure support is secure to vessel, describe any hazards. 
	
	
	
	X
	

	Nozzle Assess paint, look for leakage, and ensure stud threads are fully engaged. Record any damage, deflection, etc. Are nozzles gusseted?
	X
	
	
	
	Threaded nozzle joints are fully engaged. No leaks observed.
No damage or deflections

Nozzles are not gusseted

	Gauges Ensure gauges are visible, working, no leakage, and suitable for range of MAWP/ Temp.
	X
	
	
	
	Gauge is clear and clean. No leakage.
Suitable for range of MAWP of vessel.

Pressure gauge 0 – 1000 PSI

	External Piping Ensure pipe is well supported. All clamps, supports, shoes, etc. in place. Look for evidence of structural overload, deflection, etc. Paint condition, external corrosion?
	X
	
	
	
	Piping is well supported. All clamps and supports are in place.
No structural overloads or deflections.

Paint in good condition

	Valving Ensure no leaks are visible. Valves are properly supported and chained if necessary.
	X
	
	
	
	No leaks are visible.
Valves are supported properly

	PSV Ensure PSV is set at pressure at or below that of vessel. 
	X
	
	
	
	PSV is set at MAWP of vessel.
Discharge piping is same size as valve outlet.

PSV seal in place.

No block valve between PSV and vessel

	NDE methods Was UT/ MPI done on vessel
(MI coordinator to review results)
	X
	
	
	
	Ultrasonic thickness survey carried out – no metal thickness detected below nominal minus corrosion allowance.

	Other


	
	
	
	
	

	Recommendations or corrective actions :  Vessel is Fit for  Service or describe corrective actions required)
(MIC to review corrective actions with Operations, discuss with Chief Inspector where necessary, and get remedial action implemented)

Recommendations: No recommendations.
Summary: Vessel is in overall good condition.  Ultrasonic corrosion survey performed—no metal thickness detected below nominal minus corrosion allowance. 

Vessel is fit for service.


Inspected By: Gerry Avery


                                                                                       Date: November 8, 2007
Photo Table

	[image: image1.jpg]w I MAX. ALLOW
RT | | WORK. PRESS.
axl | MIN. DESIGN
METAL TEMP.

|
|
|
|
|

SERIAL
NO.

DESIGN
PRESS.

HEAD
MTRL.

SHELL | _ &
MTRL. ’7/\ {1 06

%)

4 E’"b&kl (

: ' X

- *“*F«'«‘u:m-

A 2w .an ®

’ ‘ ‘ :
| L1

N

~





	[image: image2.jpg]| psi

NACE MR-01-75






	vessel data plate
	vessel pressure gauge

	[image: image3.jpg]



	[image: image4.jpg]




	vessel skirt bolted to skid floor
	vessel overview

	
	

	
	


















































