	Canadian Natural Resources Limited

GENERAL PRESSURE VESSEL INFORMATION

	District:   Fort St. John, B.C.
	Skid No.    

	Facility:   Clear Hills Gas Field
	Location (LSD):  13-01-88-13-W6M 

	Vessel Name Equipment Number:  3 Phase Separator

	Orientation:  Vertical

	Status:          In Service
	   Regulatory Inspection  

	PRESSURE VESSEL NAMEPLATE DATA

	“A” or “G” or “S” (Sask.) or BC Registration Number.

A2682187
	CRN Number:

H 5173.2

	Vessel serial number:  108-18-90
	Size:  16in.x 78in.

	Shell thickness:       21.4mm
	Shell material:  SA 333-6     

	Head thickness:      22.2mm
	Head material:   SA 516-70    

	Tube wall thickness:     
	Tube material:    

	Tube diameter:    
	Tube length:        

	Channel thickness:    
	Channel material:     

	Design pressure
	Shell:     9929  kPa
	Operating pressure
	Shell:    0 – 3000 PSI    

	
	Tubes:     
	
	Tubes:     

	Design Temp.
	Shell:       38 °C
	Operating temperature
	Shell:    

	
	Tubes:       
	
	Tubes:                                                 

	X-ray:  RT2                      
	Heat treatment:   no

	Code parameters:   ASME VIII, Div 1  
	Coated:  no             

	Manufacturer:     Mar - Quinn
	Year built:  1990       

	Corrosion allowance:  1.6 mm   
	Manway:   no         

	PRESSURE SAFETY VALVE NAMEPLATE DATA

	PSV Tag  #
	Manufacture
	Model #
	Serial #
	Set Pressure

(kPa)
	Capacity

(scfm)
	Service

Date

	7723 F 
	Mercer
	8117151T17G21
	173359
	1440 PSI
	4956
	03/05

	CRN #
	Service By
	Block Valve
	Location
	Size
	Code Stamp
	

	OG8841.5C 

	Unified valve
	No 
	Upper shell
	1”x 1”
	UV
	

	SERVICE CONDITIONS-INDICATE ALL THAT APPLY

	  Sweet   
	Sour  X
	 Oil   
	Gas     
	Water  

	 Amine
	LPG    
	Condensate    
	Air  
	Glycol  

	Other (Describe):    


Inspection Interval ________________________________________PSV Service Interval_________________________________

(Determined by MIC in conjunction with Chief Inspector following guidelines of CNRL’s Owner-User Inspection Program)
Reports reviewed and accepted by:
Mechanical Integrity Coordinator________________________________________________Date__________________________

Fill out all forms as completely as possible. All information is important!  Use back of sheets to record additional information or sketch if required.

Copy of report to be filed by MIC at site, and copy sent to Chief Inspector

	External Inspection Items


	G
	F
	P
	N/A
	                    Comments



	Insulation Verify sealed around manways, nozzles, no damage present, and there is no egress of moisture.
	
	
	
	X
	Vessel not insulated

	External Condition  Assess paint condition, areas peeling, record any corrosion, damage, etc (record location, size and depth of corrosion or damage)
	X
	
	
	
	 Paint in good condition.
No metal exposed

	Leakage Record any leakage at flanges, threaded joints, weep holes on repads, etc.
	X
	
	
	
	No leaks observed

	Skirt    Assess condition of paint, fire protection, concrete. Look for corrosion, buckling, dents, etc. Look at vessel surface area near supports. Verify no signs of leakage at attachment to vessel and attachment welds are acceptable. Ground wire attached?
	X
	
	
	
	Skirt:
Skirt bolted directly to skid floor.

No buckling or dents.

No corrosion at attachment weld to vessel.

Paint in good condition.

No ground wire attached to vessel or skid 

	Anchor Bolts    Hammer tap to ensure secure. Look for cracking in treads or signs of deformation.
	X
	
	
	
	Anchor bolts are securely fastened. No deformation

	Concrete foundation Check for cracks, spalling, etc. 
	
	
	
	X
	

	Ladder / Platform    Describe general condition, ensure support is secure to vessel, describe any hazards. 
	
	
	
	X
	

	Nozzle Assess paint, look for leakage, and ensure stud threads are fully engaged. Record any damage, deflection, etc. Are nozzles gusseted?
	X
	
	
	
	Threaded nozzle joints are fully engaged.
No leaks observed.

No damage or deflections.

Nozzles are not gusseted

	Gauges Ensure gauges are visible, working, no leakage, and suitable for range of MAWP/ Temp.
	X
	
	
	
	Gauge is clear and clean. No leakage.
Suitable for range of MAWP/temperature.

Pressure gauge 0 – 3000 PSI

	External Piping Ensure pipe is well supported. All clamps, supports, shoes, etc. in place. Look for evidence of structural overload, deflection, etc. Paint condition, external corrosion?
	X
	
	
	
	Piping is well supported.
All clamps and supports are in place

No structural overloads or deflection

Paint in good overall condition

	Valving Ensure no leaks are visible. Valves are properly supported and chained if necessary.
	X
	
	
	
	No leaks are visible.
Valve supported properly

	PSV Ensure PSV is set at pressure at or below that of vessel. 
	X

	
	
	
	Located on inlet piping - set at MAWP of vessel.

	NDE methods Was UT/ MPI done on vessel
(MI coordinator to review results)
	X
	
	
	
	Ultrasonic thickness survey carried out – no metal thickness detected below nominal minus corrosion allowance.

	Other


	
	
	
	
	

	Recommendations or corrective actions :  Vessel is Fit for  Service or describe corrective actions required)
(MIC to review corrective actions with Operations, discuss with Chief Inspector where necessary, and get remedial action implemented)

Recommendations: Install ground cable.
Summary: Vessel is in overall good condition.  Ultrasonic corrosion survey performed—no metal thickness detected below nominal minus corrosion allowance. 

Vessel is fit for service.


Inspected By:   
Gerry Avery







                        Date:  June 21, 2007
	[image: image1.jpg]VSISO





	[image: image2.jpg]




	           Vessel data plate
	               Vessel pressure gauge

	[image: image3.jpg]



	[image: image4.jpg]




	                Vessel skirt bolted to skid floor
	      vessel overview

	
	

	              
	








