	Canadian Natural Resources Limited

GENERAL PRESSURE VESSEL INFORMATION

	District:   Fort St. John, B.C.
	Skid No.    

	Facility:   Clear Hill Gas Gathering
	Location (LSD): 02-13-87-13-W6M  

	Vessel Name Equipment Number:  3 Phase Separator

	Orientation:  Vertical

	Status:          In Service
	   Regulatory Inspection  

	PRESSURE VESSEL NAMEPLATE DATA

	“A” or “G” or “S” (Sask.) or BC Registration Number.

A 3174937
	CRN Number:

K 9276.21

	Vessel serial number:  60273-200
	Size:  16in. x 84in.

	Shell thickness:       26.19mm
	Shell material:      SA 106-B 

	Head thickness:      20.98mm
	Head material:      SA 516-70N

	Tube wall thickness:     
	Tube material:    

	Tube diameter:    
	Tube length:        

	Channel thickness:    
	Channel material:     

	Design pressure
	Shell:         9929 kPa
	Operating pressure
	Shell:        0 – 6800 KPa

	
	Tubes:     
	
	Tubes:     

	Design Temp.
	Shell:        38 °C
	Operating temperature
	Shell:    -40 – 50 Deg. C  

	
	Tubes:       
	
	Tubes:                                                 

	X-ray:    RT 2                       
	Heat treatment:  no 

	Code parameters:   ASME VIII, Div 1  
	Coated:    no           

	Manufacturer:  Nusco   
	Year built: 1996        

	Corrosion allowance:  1.59mm   
	Manway:  no          

	PRESSURE SAFETY VALVE NAMEPLATE DATA

	PSV Tag  #
	Manufacture
	Model #
	Serial #
	Set Pressure

(kPa)
	Capacity

(scfm)
	Service

Date

	 
	Mercer
	8112151T17G21
	23668
	9929
	4956
	03/05

	CRN #
	Service By
	Block Valve
	Location
	Size
	Code Stamp
	

	OG2606.5C 

	Unified Valve
	No
	Upper shell
	1”x 1”
	UV
	

	SERVICE CONDITIONS-INDICATE ALL THAT APPLY

	  Sweet   
	Sour  X
	 Oil   
	Gas    X 
	Water  X

	 Amine
	LPG    
	Condensate  X  
	Air  
	Glycol  

	Other (Describe):    


Inspection Interval ________________________________________PSV Service Interval_________________________________

(Determined by MIC in conjunction with Chief Inspector following guidelines of CNRL’s Owner-User Inspection Program)
Reports reviewed and accepted by:
Mechanical Integrity Coordinator________________________________________________Date__________________________

Fill out all forms as completely as possible. All information is important!  Use back of sheets to record additional information or sketch if required.

Copy of report to be filed by MIC at site, and copy sent to Chief Inspector

	External Inspection Items


	G
	F
	P
	N/A
	                    Comments



	Insulation Verify sealed around manways, nozzles, no damage present, and there is no egress of moisture.
	
	
	
	X
	Vessel not insulated

	External Condition  Assess paint condition, areas peeling, record any corrosion, damage, etc (record location, size and depth of corrosion or damage)
	X
	
	
	
	 Paint in good overall condition.


	Leakage Record any leakage at flanges, threaded joints, weep holes on repads, etc.
	X
	
	
	
	No leaks observed

	Skirt    Assess condition of paint, fire protection, concrete. Look for corrosion, buckling, dents, etc. Look at vessel surface area near supports. Verify no signs of leakage at attachment to vessel and attachment welds are acceptable. Ground wire attached?
	X
	
	
	
	Skirt:
Skirt welded directly to skid floor.

No buckling or dents.

No corrosion at attachment welds to vessel.

Corrosion on skirt at floor level.

No ground wire attached to vessel or skid

	Anchor Bolts    Hammer tap to ensure secure. Look for cracking in treads or signs of deformation.
	
	
	
	X
	Skirt welded to skid floor

	Concrete foundation Check for cracks, spalling, etc. 
	
	
	
	X
	

	Ladder / Platform    Describe general condition, ensure support is secure to vessel, describe any hazards. 
	
	
	
	X
	

	Nozzle Assess paint, look for leakage, and ensure stud threads are fully engaged. Record any damage, deflection, etc. Are nozzles gusseted?
	X
	
	
	
	Threaded nozzle joints are fully engaged.
No leaks observed.

No damage or deflections

Nozzles are not gusseted

	Gauges Ensure gauges are visible, working, no leakage, and suitable for range of MAWP/ Temp.
	X
	
	
	
	Gauges are clear and clean. No leakage.
Not suitable for range of MAWP/ Temperature.

Pressure gauge 0 – 6800 KPa/ temperature gauge -40 – 50 Deg. C

	External Piping Ensure pipe is well supported. All clamps, supports, shoes, etc. in place. Look for evidence of structural overload, deflection, etc. Paint condition, external corrosion?
	X
	
	
	
	Piping is well supported. All clamps and supports are in place.
No structural overloads or deflection.

Paint peeling to 45 % of area.

Corrosion on piping no pitting

	Valving Ensure no leaks are visible. Valves are properly supported and chained if necessary.
	X
	
	
	
	No leaks are visible.
Valves are properly supported

	PSV Ensure PSV is set at pressure at or below that of vessel. 
	X

	
	
	
	Located on upper shell - set at MAWP of vessel.

	NDE methods Was UT/ MPI done on vessel
(MI coordinator to review results)
	X
	
	
	
	Ultrasonic thickness survey carried out – no metal thickness detected below nominal minus corrosion allowance. 

	Other


	
	
	
	
	

	Recommendations or corrective actions :  Vessel is Fit for  Service or describe corrective actions required)
(MIC to review corrective actions with Operations, discuss with Chief Inspector where necessary, and get remedial action implemented)

Recommendations: Attach ground wire to skid
Summary: This Vessel is in good overall condition, ultrasonic thickness survey carried out – no metal thickness detected below nominal minus corrosion allowance.

Vessel is fit for service                                                                                                                                                                                                                                


Inspected By:  Gerry Avery      



                                                                                 Date:  June 18, 2007
	[image: image1.jpg]CERTIFIED BY

NUSCO

NISKU, ALBERTA, CANADA

MAX. ALLOW
WORK. PRESS.

o




	[image: image2.jpg]




	            Vessel data plate
	              Vessel temperature gauge

	[image: image3.jpg]716 58
TUBE AND CONNECTION

kPa

M’

psi

NACE MR-01-75





	[image: image4.jpg]5 2
e ” e o i # 7 &
-
- 4
e
e
-
.
#
F ad »
4
* 2
~ o
E -~ g >
” -
o L4 7
v g 4 / Foow
£ ; -






	             Vessel pressure gauge
	        Vessel skirt welded to skid floor

	[image: image5.jpg]



	

	       Vessel overview
	








