

**INSPECTION FILE REVIEW AND FITNESS FOR SERVICE DETERMINATION.**

**LH-0033 Line Heater**

**Inspection Report for:** LH-0033 - Coil 1

**Remaining Life:** 10 YRS **Date of this Report:** 09/11/2018

**Average Corrosion Rate:** 22 MPV **Next UT:** 09/11/2021 **Next VT:**

**Manufacturer:** DynaCorp Fabricators **Mfg Serial #:** 6J111050

**Date Built:** 2012 **National Board #:** None

09/11/2021

**Alberta registration #:** 617901 **Canadian Registration #:** T9862.2

I reviewed the inspection file to determine if a 3-year inspection frequency was adequate.

After reviewing the data, I found that the unit is fit for continued service until the next scheduled inspection in 2021.

I have changed the Last Eaton report to reflect this three year frequency.

Notes:

1. the UT data in the current report needs to be updated with correct data, Tmin, nominals, etc.
2. I have made modifications to the report changing the report from a 1 year frequency to a 3 year frequency to reflect the next inspection date to 09/11/2021

Steven Theobald

TechnipFMC U.S. Flow Testing Service

 Integrity Manager | Surface America